Supporting Information

Towards Efficient and Industrially Compatible Fully-Textured Perovskite Silicon Tandem Solar Cells: Controlled Processing and Understanding of Perovskite Formation

O. Er-raji*, A. J. Bett, S. Lange, H. Nagel, M. Bivour, O. Schultz- Wittmann, C. Hagendorf, M. Hermle, J. Borchert, S. W. Glunz, P. S. C. Schulze

Figure S1. Influence of the co-evaporation precursors and the organohalide solution mixture on the perovskite absorber’s absorptance, reflectance and transmittance.  a), d), g), j) Absorptance, b), e), h), k) reflectance and c), f), i), l) transmittance as a function of the organohalide mixture (FABr/FAI) spincoated on top of four different scaffolds with either CsI or CsBr as co-evaporation precursor with PbI2 (CsX:PbI2 = 12% or 15% rate ratio, X = I or Br). A downwards shift in the reflection pattern can be observed for all 4 variations when the FABr/FAI ratio is ≤ 50/50.

Figure S2: Impact of the organohalide mixture on the perovskite layer morphology. Top-view SEM images of perovskite absorbers with a bandgap of 1.66 eV (estimated by the PL peak position) processed with an organohalide mixture of FABr/FAI = 65/35 and a CsI to PbI2 evaporation rate ratio of a) 10%, b) 12% and c) 15%; or an organohalide mixture of FABr/FAI = 50/50 and a CsBr to PbI2 evaporation rate ratio of e) 10%, f) 12% and g) 15%. A dendritic perovskite film formation can be noted when the solution mixture is inside the critical regime (FABr/FAI ≤ 50/50).

Figure S3: Impact of the organohalide mixture on the perovskite structural quality. XRD measurements of perovskite absorbers synthesized on a) flat substrates and b) textured substrates, with a variation in organohalide solution mixture and evaporated cesium halide (either CsBr or CsI, with PbI2). All perovskite compositions do not show an additional phase besides the perovskite cubic phase and PbI2 phase on flat substrates.

Figure S4: Impact of the substrate roughness on the perovskite phase purity. XRD measurements of perovskite absorbers synthesized on a flat substrate (grey) and a textured substrate (red). Besides the perovskite cubic phase, a PbI2 can be detected on the flat substrate while no impurities are detected on the textured substrate.

Figure S5. Impact of the substrate (planar vs textured) on the halide and A+ cation ratio of the perovskite absorber. a) Iodide to bromide ratio, b) cesium to lead ratio, and c) sum of carbon and nitrogen to cesium ratio for perovskite absorbers formed on top of a flat vs a textured substrate, derived via XPS depth profiling measurements through the layer stack.

Figure S6. Influence of substrate rotation during ToF-SIMS measurements on the elemental composition of perovskite. ToF-SIMS measurements for a perovskite absorber deposited on a) a flat substrate and b) a textured substrate. A dependence of the measurement on the substrate rotation can be seen only for the textured substrate.

Figure S7. Localization of remnant PbI2 in perovskites processed on textured silicon. a) Schematic of the probed architecture with textured silicon as a substrate and Perovskite/2PACz/ITO layers on top. b) Cross-section SEM image of a perovskite absorber formed on textured silicon with an organohalide solution concentration of 0.67M; the red arrows indicated remnant PbI2 at the interface with the underlying charge transport layer. c) XRD measurements of perovskite absorbers formed on textured silicon with a variation in the organohalide solution concentration. The performed measurements show the tendency of PbI2 accumulation at the bottom perovskite interface in case of non-balance between evaporated inorganic compounds and wet-chemically deposited organic precursors.

Figure S8. Impact of evaporation rate ratio on scaffold composition. XPS measurements (with ion etching along the depth) of evaporated CsI/PbI2 layers with a variation in the rate ratio (10% grey, 12% red and 15% blue). The PbI2 rate is set to 1 Å s-1. With higher rate ratio, the measured atomic cesium in the scaffold is increased.

Figure S9. Impact of organohalide solution deposition speed (to control perovskite phase purity) on single junction perovskite solar cell parameters. a) Photograph of a glass substrate with four active cell areas (0.25 cm²). (b) Schematic structure of an opaque single-junction solar cell. Photovoltaic parameters c) jSC, d) VOC, e) FF and f) PCE of perovskite single-junction solar cells with a variation in organohalide deposition speed. Forward and reverse jV curves of the best performing device from each variation: g) 1000 rpm, h) 2200 rpm, i) 3000 rpm and j) 4000 rpm. A low performance is observed for the variations with extreme deposition speeds (1000 rpm and 4000 rpm).

Figure S10. Performance and stability of a perovskite single junction solar cell without impurities in the perovskite absorber. a) Forward and reverse jV curves of the best performing device. b) Normalized maximum power point, voltage and current, and c) stage temperature, chamber temperature, and relative humidity during the 100-hour stability test. A good performance and stability of the device is achieved.

Figure S11. PL and XRD characteristics of perovskite absorbers formed on textured silicon with a variation in organohalide solution deposition speed. a) PL peak position, b) perovskite (100) main XRD peak and c) its respective FWHM, of perovskite absorbers formed on textured silicon with a variation in organohalide solution deposition speed. No large change can be seen depending on the variation.

Figure S12. LEXT optical microscope characterization of the front silicon texture pattern. a) LEXT microscope image of an area of a textured silicon bottom cell with random pyramid texture. b) and c) pyramid size distribution extracted from the LEXT image.

Figure S13. Fully-textured perovskite silicon tandem solar cell. a) Photograph of the tandem solar cell with an active area of 1 cm². b) Stabilized power conversion efficiency of the tandem cell measured at a fixed voltage close to the maximum power point. A stable power output of 26.5% is recorded.

(d)

(d)

(c)

(c)

(a)

(a)

(b)

(b)

Figure S14. Statistics on fully-textured perovskite silicon tandem solar cells performance. Box plots presenting a) jSC, b) VOC, c) FF, and d) PCE metrics extracted from jV measurements. Beside outliers, the efficiency within the batch is within 1.5%abs PCE range difference.