Glycosaminoglycans exhibit distinct interactions and signaling with BMP2 according to their nature and localization

Jean Le Pennec1, Olga Makshakova2,3, Paola Nevola1,4, Farah Fouladkar1, Evelyne Gout5, Paul Machillot1, Mélanie Friedel-Arboleas5, Catherine Picart1, Serge Perez6, Andrea Vortkamp7, Romain R. Vivès5*, Elisa Migliorini1*

1Univ. Grenoble Alpes, INSERM, CEA, CNRS, U1292 Biosanté, EMR 5000, Grenoble, France

2Faculty of Biology, University of Freiburg, 79104 Freiburg, Germany.

3Signalling Research Centres BIOSS and CIBSS, Synthetic Biology of Signalling Processes lab, University of Freiburg, 79104 Freiburg, Germany

4Dipartimento di Ingegneria Chimica dei Materiali e della Produzione Industriale, University of Naples Federico II, Napoli, Italy.

5 Univ. Grenoble Alpes, CNRS, CEA, IBS, Grenoble, France

6 Univ. Grenoble Alpes, CNRS, Centre de Recherche sur les Macromolécules Végétales, Grenoble, France

7Developmental Biology, Centre for Medical Biotechnology, University Duisburg-Essen, Essen, Germany.

*Co-Corresponding authors

Migliorini Elisa (E.M.): elisa.migliorini@cea.fr

Romain Vivès (R.R.V.): romain.vives@ibs.fr

Supporting information

Methods

Western Blot

800 000 serum-starved cells were seeded onto 24x24 mm gold surfaces, functionalized with biomimetic platforms as previously described, disposed in wells of 6-well plates (Corning), and incubated for 90 min at 37°C and 5% CO2. Then they were rinsed with ice-cold PBS, and lysed with RIPA lysis buffer (Sigma-Aldrich) and scraped. The samples were centrifuged at 1600 rpm for 20 min at 4°C. The proteins were quantified using BCA assay (Sigma-Aldrich). Laemmli SDS sample buffer 4X (ThermoFisher Scientific) was added to the samples. For each sample, 8 µg of total protein was loaded in precast polyacrylamide gel (4561023, Bio-Rad) and protein migration was achieved by electrophoresis with Mini-PROTEAN Tetra Cell (Bio-Rad) in running buffer (25 mM Tris, 190 mM glycine, 0.1% (v/v) SDS in MilliQ water) according to standard protocols.

The proteins were then transferred to a PVDF (polyvinylidene difluoride) membrane using iBlot™ 2 Dry Blotting System (Bio-Rad Laboratories), rinsed with TBS-T (20 mM Trizma® base, 150 mM NaCl and 0.1% (v/v) Tween-20 at pH 7.5), blocked with 5% BSA in TBS-T and kept in constant agitation for 1 hour. Blocked membrane was probed with rabbit anti-pSMAD1/5/9 (1:1000 Cell Signaling Technology) and rabbit anti-GADPH (1:2000, Cell Signaling Technology) as a reference in 3% BSA in TBS-T and kept on constant agitation overnight at 4°C. Immunological detection was achieved with anti-rabbit HRP-conjugated secondary antibody (1:5000, ThermoFisher Scientific). The proteins were visualized by chemiluminescence on an iBright FL1000 Imaging System (ThermoFisher Scientific) using a Clarity™ Western ECL Substrate (Bio-Rad Laboratories). pSMAD1/5/9 was quantified with ImageJ and was normalized by GAPDH control.

Separation of glycosaminoglycan with PAGE

The separation of GAGs based on their size was achieved with polyacrylamide gel electrophoresis (PAGE)[49]. Initially, 10 μg of samples diluted in 20% glycerol were run through a 1.5 cm stacking gel (1 M Tris/HCl, pH 6.8, 5% acrylamide, 2% cross-linker) at a constant voltage of 150 V for 1 h in running buffer (Tris-HCl 2.5 mM, glycine 20 mM). Then samples were passed through the resolving gel (1.5 M Tris/HCl at pH 8.8, 25% acrylamide and 5% cross-linker) with a constant current of 25 mA for 3 h (maximum voltage of 1000 V). A mixture of Xylene Cyanole, Bromophenol Blue and Phenol Red in 20% glycerol was used in a separate lane as electrophoresis markers. After electrophoresis, GAG bands were visualized by staining with 0.08% aqueous Azure A for 10 min under constant agitation. The gel was washed twice in water for 5 min to remove the excess of dye.

Extraction, purification and structural analysis of GAGs from CHO cells

GAGs were isolated and purified, as described (Henriet et al., 2017). Briefly, cells were digested with trypsin (45 min at 37°C), followed by centrifugation to remove cell debris. Supernatants were recovered, supplemented with 2 mM MgCl2, and treated with 250 U/µL Benzonase (Merck) and for 2 h at 37°C. After heat inactivation (96°C, 5 min) and centrifugation, GAGs were isolated from the supernatants by weak anion exchange chromatography, using a DEAE-Sephacel column (Pharmacia Biotech) equilibrated in 20 mM phosphate pH 6.5. The column was first washed with 20 mM phosphate pH 6.5, 0.3 M NaCl, then GAGs were eluted with 20 mM phosphate pH 6.5, 1 M NaCl. Samples were desalted over a Pd-10 column (GE Healthcare), lyophilized, and stored at -20°C prior to analysis. For quantification of HS, samples were digested with a mix of heparinase I, II and III (10 mU each) in 100 mM sodium acetate, 0.5 mM calcium acetate, pH 7.1 (48 h, 37°C), and disaccharide products were identified and quantified by RPIP-HPLC, coupled to on-line post-column disaccharide 2-cyanoacetamide derivatization, and calibrated with commercial standards (Iduron), as previously described (Laguri, Sadir, Gout, Vivès, & Lortat-Jacob, 2022). similarly, quantification of CS was achieved by digesting samples with Chondroitinase ABC (100 mU) in 50 mM Tris-HCl pH 7.5, 50 mM NaCl, 2 mM CaCl2 (24 h, 37°C), followed by RPIP-HPLC analysis.

Supplementary results

Supplementary table 1. Kinetics parameters determined via BLI for the interactions of BMP2 with various GAGs. Background in darker blue indicates a stronger interaction. Data are represented as mean ± SEM for at least two independent experiments.

|  | KD (µM) | kon (1/Ms) (103) | koff (1/s) (10-2) |
| --- | --- | --- | --- |
| HS | 0.057±0.007 | 300±33 | 2±0.01 |
| HA |  |  |  |
| CS-A | 74±23 | 1±0.7 | 10±4 |
| CS-D | 0.40±0.04 | 134±18 | 5±1 |
| CS-E | 2.5±0.4 | 37±3 | 9±1 |
| DS | 1.4±0.4 | 97±24 | 12±1 |

| CS-A |  |  |  |
| --- | --- | --- | --- |
| CS-D |  |  |  |
| CS-E |  |  |  |
| DS |  |  |  |
| HS |  |  |  |
| HA |  |  |  |

Figure Si1. Raw data for all replicates of BLI kinetics assays of BMP2 binding on different GAGs: CS-A, CS-D, CS-E, DS, HS and HA (binding not detected). On HA, the BLI data gave negative and comparable adsorption as in the SAv reference chip. The phases of BMP2 association and dissociation were measured for 200s each at different concentrations indicated at the bottom of each graph (nM). The curves were fitted with a 1:1 Langmuir binding model on the full association and 40 s of the dissociation (red curves), with the exception of HA (no binding detected),to obtain the kinetics parameters of the interactions.

Figure Si2. Acrylamide gel electrophoresis of the different GAGs for relative comparison of molecular weights (with the approximation of the global charge impact).

Figure Si3. QCM-D study of the interaction between GAGs and BMP2. A: desorption of BMP2 from all the tested GAGs. B-C Plots of D versus -f for the B. immobilization of GAGs on SAv and C binding of BMP2 on the different GAGs. -f corresponds to the hydrated mass bound on the surface and D corresponds to the mechanical properties of the deposited molecule film (rigidity, crosslinking). We notice that the mechanical properties of the different GAGs are not comparable upon binding of BMP2. BMP2 increased more the rigidity of the HS and DS films compared to the other GAGs, in particular CS-D.

Figure Si4. Co-functionalization process to build biomimetic platforms presenting cRGD peptides, GAGs and BMP2 for cellular assays. A. Schematic representation of the biomimetic platforms presenting cRGD, GAGs and BMP2. The sequential buildup of the platforms was characterized via QCM-D for B. HS, C. CS-A and D. CS-D. The cRGD peptide was injected at 0.5 µg/mL at 100 µL/min until reaching a frequency shift of -4.7 Hz. This shift was determined by mimicking the liquid-handling robot functionalization with a “fast injection” procedure at 100 µL/min followed by 10 min static incubation. Since the follow-up rinsing always led to additional binding of cRGD remaining in the tubing, we chose this lower concentration of 0.5 µg/mL with respect to the 1.2 µg/mL used for the liquid-handling robot to allow a better control. The * symbol corresponds to a transition in Hepes-T before the BMP2 injection at 5 µg/mL. In comparison to the platform without cRGD (Figure 2) , the frequency shift upon BMP2 binding was increased on HS and CS-D while it was reduced on the CS-A platform. With the co-functionalization procedure, the number of available biotin binding sites for the GAGs was decreased about 65-75%. The reduced GAG density on the platforms may modify the binding dynamics by reducing cross-linking and facilitating the BMP2 binding to intra-chain regions. Overall, the binding of BMP2 detected via QCM-D on the biomimetic platforms was stronger on CS-D and CS-E than on DS, HS and CS-A.

Figure Si5. A. Quantification of cell-surface HS and CS levels on CHO WT and mutants by disaccharide analysis (n=2).
B. Quantification of the mean immunofluorescence intensity of pSMAD1/5/9 translocated in the nuclei of CHO wild type and mutants in identical experiment. Values were normalized by the positive sBMP2 positive control (n=4). Statistical significance between two conditions was tested with Mann-Whitney test and was represented with * for p ≤ 0.05.
C. Western blot of pSMAD1/5/9 levels of CHO WT and the mutants KO HS and KO HS/CS cells cultured for 90 min on cRGD biomimetic platforms with or without sBMP2 at 0.1 µg/mL. 
D. Quantification of the Western Blot bands. pSMAD1/5/9 was normalized by GAPDH.

Figure Si6: BMP2 can bind to short HS oligosaccharides as short as HS-dp4 and induce p-SMAD1/5/9 signaling.
 a) QCM-D characterization of the binding BMP2 to of full chain HS and HS-dp of different length (dp4, 8 and 12). Frequency shifts are plotted over the time. Starting and duration of incubation steps are indicated by arrows; during the other times, surfaces were exposed to working buffer. b, c) C2C12 were plated on platforms characterized with QCM-D and lysed after 60 minutes. The expression of phosphorylated SMAD 1/5/9 has been analyzed by western blot and quantified relative to GAPDH expression (loading control) in panel c (n=3).

Figure Si7. Generation of the HS-oligosaccharide library. A. Size exclusion chromatography of HS fragmented by heparinase III digestion. The absorbance at 232 nm detects the unsaturated bonds generated by heparinase III cleavage. Collected tetrasaccharides and hexasaccharides are represented in red. B and C. Absorbance measurement to detect the elution and separation of HS tetrasaccharides and hexasaccharides, respectively, by SAX-HPLC. The different peaks represented by letters (B to AC) were collected and their disaccharide composition was determined by RPIP-HPLC. Letters in red represent the selected oligosaccharides that were biotinylated to perform binding analysis with BMP2.

| HS-dp6 |  |
| --- | --- |
| A Batch1 |  |
| B Batch 3 |  |
| C Batch 3 |  |
| D Batch1 |  |
| E Batch 4 |  |
| F Batch 3 |  |
| G Batch 3 |  |
| H Batch 3 |  |
| I Batch 2 |  |
| J Batch 2 |  |
| K Batch 2 |  |
| L Batch 4 |  |
| M Batch 2 |  |
| N Batch 3 |  |
| O Batch 2 |  |
| P Batch 4 |  |
| Q Batch 3 |  |
| R Batch1 |  |
| S Batch 3 |  |
| T Batch 4 |  |
| U Batch1 |  |
| V Batch 3 |  |
| W Batch 3 |  |
| X Batch 2 |  |
| Y Batch 3 |  |
| Z Batch1 |  |
| AA+ AB Batch 2 |  |
| AC Batch2 |  |

| HS-dp4 |  |
| --- | --- |
| A Batch 2 |  |
| B Batch 3 |  |
| C Batch 3 |  |
| D Batch 3 |  |
| E Batch 3 |  |
| F Batch 2 |  |
| G Batch 4 |  |
| H Batch 4 |  |
| I Batch 3 |  |
| J Batch 4 |  |
| K Batch 3 |  |
| L Batch 3 |  |
| M Batch 2 |  |
| N Batch 4 |  |
| O Batch 3 |  |
| P Batch1 |  |
| Q Batch 3 |  |
| R Batch2 |  |
| S Batch1 |  |
| T Batch 3 |  |
| U Batch 3 |  |
| V Batch 3 |  |
| W Batch 3 |  |
| X Batch 3 |  |
| Y Batch1 |  |
| Z Batch2 |  |
| AA Batch 3 |  |
| AB Batch1 |  |
| AC Batch 3 |  |
| AD Batch 2 |  |
| AE Batch2 |  |
| AF Batch 4 |  |
| AG Batch 3 |  |
| AH Batch 2 |  |
| AI Batch 3 |  |
| AJ Batch 3 |  |
| AK Batch 3 |  |
| AL Batch 2 |  |
| AM Batch 3 |  |

| HS disaccharide standards |  |
| --- | --- |
| Mix HS Batch 1 |  |
| Mix HS Batch 2 |  |
| Mix HS Batch 3 |  |
| Mix HS Batch 4 |  |

Figure  Si8. Disaccharide composition profile of the entire oligosaccharide library. After digestion with a cocktail of heparinase I, II and III, the oligosaccharides are cleaved into disaccharides that are separated, labelled and detected using a RPIP-HPLC setup, calibrated with HS disaccharide standards to identify detected disaccharide structures. For each experiment (called batch), at least one sample composed of standard disaccharides was injected (see above). It is common to observe a peak at 17’ that might correspond to an isomeric structure of ∆UA–GlcNS disaccharide but the unambiguous elution times of standard disaccharides are as follows:

| 16’ | 20’ | 22’-24’ | 24’-26’ | 33’-36’ | 36’-40’ | 43’-47’ | ~57’ |
| --- | --- | --- | --- | --- | --- | --- | --- |
| ∆UA–GlcNAc | ∆UA–GlcNS | ∆UA– GlcNAc6S | ∆UA2S – GlcNAc | ∆UA – GlcNS6S | ∆UA,2S – GlcNS | ∆UA,2S – GlcNAc,6S | ∆UA2S – GlcNS6S |

The different peaks were integrated and signal / mass ratio corrections were applied to determine the amounts of each disaccharide. By summing the amounts of disaccharide components for each oligosaccharide, we could determine the quantities produced for the entire oligosaccharide library.

| dp4-P |  |  |  |
| --- | --- | --- | --- |
| dp4-S |  |  |  |
| dp4-Y |  |  |  |
| dp4-AB |  |  |  |
| dp6-D |  |  |  |
| dp6-I |  |  |  |
| dp6-J |  |  |  |
| dp6-K |  |  |  |
| dp6-L |  |  |  |
| dp6-P |  |  |  |
| dp6-Q |  |  |  |
| dp6-R |  |  |  |
| dp6-S |  |  |  |
| dp6-U |  |  |  |
| dp6-Z |  |  |  |
| dp6-AC |  |  |  |

Figure Si9. Raw data for all replicates of BLI kinetics assays of BMP2 binding on different HS oligosaccharides. The phases of BMP2 association and dissociation were measured for 200 s each at different concentrations indicated at the bottom of each graph (nM). The curves were fitted with a 1:1 Langmuir binding model on the full association and 40 s of the dissociation (red curves) to obtain the kinetics parameters of the interactions.

| HS-dp6 |  |
| --- | --- |
| D structure |  |
| D |  |
| D NaBH4 |  |
| E structure |  |
| E |  |
| E NaBH4 |  |
| G structure |  |
| G |  |
| G NaBH4 |  |
| I structure |  |
| I |  |
| I NaBH4 |  |
| J structure |  |
| J |  |
| J NaBH4 |  |
| K structure | Major Minor |
| K |  |
| K NaBH4 |  |
| L structure |  |
| L |  |
| L NaBH4 |  |
| P structure |  |
| P |  |
| P NaBH4 |  |
| Q structure |  |
| Q |  |
| Q NaBH4 |  |
| R structure | Major Minor |
| R |  |
| R NaBH4 |  |
| S structure |  |
| S |  |
| S NaBH4 |  |
| U structure |  |
| U |  |
| U NaBH4 |  |
| Z structure |  |
| Z |  |
| Z NaBH4 |  |
| AC structure | + unidentified compound |
| AC |  |
| AC NaBH4 |  |

| HS-dp4 |  |
| --- | --- |
| P structure |  |
| P |  |
| P NaBH4 |  |
| S structure |  |
| S |  |
| S NaBH4 |  |
| Y structure |  |
| Y |  |
| Y NaBH4 |  |
| AB structure | Major Minor |
| AB |  |
| AB NaBH4 |  |

Figure Si10. RPIP-HPLC disaccharide analysis of oligosaccharides with or without NaBH4 reduction. The comparison of both analyses allow determining the reducing end of the oligosaccharides (lacking in the analysis with NaBH4). Generally, the sequence of the different oligosaccharides could be determined from the substrate specificities of heparinase III for GlcNAc±6S-GlcA and GlcNS±6S-GlcA linkages. For each compound, the determined structure is first depicted, then the disaccharide analysis of the oligosaccharide, and finally the disaccharide analysis of the oligosaccharide reduced with NaBH4. The disaccharides corresponding to detected peaks are depicted in the HPLC profiles with the Symbol Nomenclature for Glycans (SNFG, Version 1.5).

Supplementary table 2. Composition of the different GAG chains determined by RPIP-HPLC disaccharide analysis.

|  | CS-A | CS-D | CS-E |
| --- | --- | --- | --- |
| 0S (0/i0) | 8,7 | 18,1 | 4,2 |
| 4S (A/iA) | 63,6 | 19,7 | 20,0 |
| 6S (C/iC) | 27,7 | 33,0 | 56,3 |
| 2S (U/iU) | 0,0 | 0,0 | 0,0 |
| 6S4S (E/iE) | 0,0 | 0,0 | 19,5 |
| 4S2S | 0,0 | 0,0 | 0,0 |
| 6S2S (D/iD) | 0,0 | 29,2 | 0,0 |
| 2S4S6S (T/iT) | 0,0 | 0,0 | 0,0 |

Figure Si11. Side (A) and top (B) view of BMP2 dimer in cartoon representation. Globular part (pdb: 6omn) of two subunits are shown in magenta and blue. For flexible N-terminal ends of the subunits, the superimposition of conformations they adopt in the course of aMD trajectory is given with relative color coding in pink and turquoise.

Figure Si12. Superimposition of docking poses of dp4-HS to BMP2 dimer with N-terminal ends truncated (pdb: 6omn). Side (A) and top (B) view. Two subunits of BMP2 are shown is pink and turquoise. Ligand’s C atoms are shown in different colors to distinguish docking poses – green, lime, plum, maroon, light blue, O atoms – red, N – blue, S – yellow.

Figure Si13. Side (A) and top (B) view of the complex between dp6-HS and BMP2 dimer with N-terminal ends truncated equilibrated in the course of MD trajectory. Two subunits of BMP2 are shown is pink and turquoise. Ligand’s C atoms are shown in green, O atoms – red, N – blue, S – yellow.

Figure Si14. The most energy favorable complex of the full-length BMP2 dimer and dp6-I equilibrated in the course of aMD trajectory: side view (A) and top view (B). Two subunits of BMP2 are shown as cartoons in pink and turquoise, semi-transparent surface of the whole protein is given in grey in contrast to representation in Figure 5, where the surface is shown only for the globular part of the protein. The same complex zoomed on the ligand (C). Surface of the globular part of BMP2 is shown in gray, the N-terminal tails are shown as cartoons in pink and turquoise colors to distinguish two subunits. The basic residues of N-terminal ends of BMP2 interacting with dp6-I (D). Shortest contacts are indicated by dashed lines. Ligand’s C atoms are shown in green, O atoms – red, N – blue, S – yellow.

Figure Si15. Binding energies in the complexes of full-length BMP2 dimer and dp6-HS (I and J) equilibrated in the course of aMD trajectories. Numbers 1 to 4 relate to four different orientations of the ligand.

Supplemenraty table 3. Per-residue contacts between BMP2 and dp6-HS ligands (with the cut-off 0.5 nm) in the course of molecular dynamics trajectories.

| Subunit 1 |  |  | Subunit 2 |  |  |
| --- | --- | --- | --- | --- | --- |
|  | Distance, nm | Standard deviation, nm |  | Distance, nm | Standard deviation, nm |
| dp6_I |  |  |  |  |  |
| Complex 1 |  |  |  |  |  |
| Arg9 Arg7 Gln1 Ser72 Lys11 Lys73 His44 Glu46 Gly45 Gln6 Ser12 Leu10 Asn71 Lys76 Lys5 Asn68 Lys8 Ser13 Ile74 Lys15 Val70 | 0.188 0.193 0.194 0.200 0.216 0.220 0.233 0.235 0.255 0.260 0.303 0.352 0.369 0.384 0.408 0.436 0.436 0.439 0.470 0.491 0.494 | 0.016 0.033 0.029 0.024 0.093 0.058 0.037 0.032 0.047 0.053 0.113 0.178 0.122 0.116 0.130 0.059 0.090 0.189 0.086 0.199 0.189 | Arg7 Arg9 Lys8 Gln6 Lys5 Lys3 His44 Pro75 Leu10 Lys73 | 0.228 0.273 0.280 0.353 0.491 0.509 0.526 0.529 0.579 0.633 | 0.072 0.181 0.164 0.147 0.237 0.348 0.224 0.175 0.253 0.283 |
| Complex2 |  |  |  |  |  |
| Arg7 Leu10 Lys76 Ser12 Lys11 Lys8 Lys73 Arg9 Gln6 Pro75 Lys5 Glu46 Ser72 Ile74 His4 Asn68 | 0.178 0.195 0.195 0.197 0.202 0.205 0.211 0.242 0.243 0.276 0.288 0.385 0.399 0.427 0.447 0.497 | 0.008 0.016 0.018 0.034 0.027 0.049 0.025 0.018 0.021 0.024 0.114 0.039 0.033 0.049 0.218 0.038 | Arg9 Lys3 Lys5 Arg7 Gln1 His44 His4 Tyr42 Ala2 Lys15 His17 Gln6 Glu46 | 0.181 0.182 0.196 0.199 0.201 0.206 0.207 0.207 0.217 0.246 0.264 0.332 0.441 | 0.008 0.012 0.017 0.023 0.014 0.016 0.020 0.032 0.015 0.124 0.042 0.049 0.027 |
| Complex3 |  |  |  |  |  |
| Ser13 Arg9 Arg7 Lys11 Leu10 Ser12 Glu46 Lys73 Ser72 His44 Gly45 Lys15 Gln6 Lys5 Pro75 Cys14 Asn71 Lys76 Lys8 Asn68 | 0.184 0.185 0.187 0.192 0.212 0.215 0.218 0.222 0.225 0.231 0.234 0.236 0.262 0.271 0.372 0.387 0.404 0.415 0.451 0.470 | 0.016 0.012 0.016 0.015 0.023 0.014 0.029 0.021 0.022 0.038 0.020 0.049 0.022 0.115 0.055 0.025 0.085 0.097 0.053 0.044 | Lys8 Arg9 Arg7 Lys11 Leu10 Gln6 Lys3 His44 Gln1 | 0.192 0.198 0.199 0.200 0.203 0.218 0.269 0.324 0.453 | 0.0092 0.0188 0.01881 0.02122 0.0142 0.03171 0.1611 0.08067 0.18726 |
| Complex4 |  |  |  |  |  |
| Arg9 Ser12 Leu10 Lys11 Lys73 Arg7 Lys8 Ser72 Pro75 Ile74 Ser13 | 0.184 0.189 0.220 0.225 0.226 0.232 0.236 0.249 0.348 0.455 0.459 | 0.011 0.025 0.039 0.036 0.022 0.061 0.067 0.029 0.079 0.043 0.049 | Lys8 Arg9 Gln6 Arg7 His44 Lys5 Gln1 Leu10 | 0.191 0.192 0.198 0.226 0.235 0.274 0.479 0.489 | 0.015 0.010 0.019 0.041 0.040 0.106 0.257 0.047 |
| dp6_J |  |  |  |  |  |
| Complex1 |  |  |  |  |  |
| Arg9 Arg7 Lys73 Glu46 Ser12 Gln6 His44 His4 Ser72 Pro75 Leu10 Ser13 Gly45 Ile74 Lys11 His17 Asn68 Lys15 Tyr42 Lys76 Lys5 | 0.187 0.188 0.205 0.212 0.217 0.222 0.227 0.228 0.245 0.253 0.285 0.296 0.303 0.356 0.360 0.395 0.398 0.399 0.403 0.407 0.422 | 0.011 0.015 0.031 0.024 0.036 0.039 0.029 0.069 0.054 0.035 0.069 0.117 0.077 0.045 0.081 0.141 0.066 0.174 0.102 0.039 0.147 | Lys3 Lys8 Arg9 Arg7 Gln6 His44 Leu10 Lys11 Gln1 Tyr42 Ser12 | 0.184 0.185 0.186 0.195 0.195 0.256 0.263 0.280 0.398 0.399 0.532 | 0.012 0.015 0.011 0.019 0.026 0.063 0.089 0.127 0.130 0.095 0.142 |
| Complex2 |  |  |  |  |  |
| Arg7 Lys76 Lys8 Leu10 Ser12 Lys3 Lys73 Lys11 Gln6 Arg9 Ala2 Cys47 Pro75 Ser72 Ile74 His4 Glu46 Gln1 Lys5 Asn68 | 0.175 0.192 0.194 0.197 0.215 0.217 0.221 0.230 0.241 0.243 0.257 0.300 0.315 0.325 0.353 0.374 0.381 0.426 0.440 0.457 | 0.007 0.016 0.029 0.014 0.054 0.029 0.023 0.103 0.016 0.025 0.029 0.057 0.055 0.092 0.079 0.026 0.037 0.143 0.048 0.029 | Lys3 Arg9 Arg7 His4 Lys5 Lys8 Ala2 Gln1 His44 Tyr42 His17 Gln6 Ser13 Pro18 Glu46 Lys15 | 0.178 0.179 0.189 0.196 0.198 0.199 0.205 0.207 0.208 0.214 0.256 0.282 0.342 0.413 0.415 0.490 | 0.014 0.009 0.016 0.013 0.015 0.018 0.018 0.039 0.023 0.032 0.026 0.031 0.108 0.093 0.052 0.120 |
| Ccomplex3 |  |  |  |  |  |
| Ser72 Lys73 Cys79 Gln1 Arg9 Lys5 Cys78 Glu46 Asn71 Ala2 Gly45 His4 Arg7 His44 Lys76 Asn68 Lys3 Val70 Cys43 Pro75 Ile74 | 0.189 0.217 0.225 0.229 0.243 0.249 0.258 0.267 0.283 0.287 0.296 0.331 0.376 0.377 0.391 0.414 0.416 0.419 0.452 0.495 0.496 | 0.018 0.045 0.068 0.137 0.177 0.140 0.054 0.052 0.075 0.165 0.066 0.257 0.192 0.127 0.107 0.072 0.189 0.146 0.076 0.040 0.045 | Arg7 Gln6 Lys11 Glu46 Ser12 Lys3 Lys76 Cys78 Gly45 His44 Leu10 Arg9 Pro75 Ala77 Gln1 Cys79 Cys47 Gln64 Lys5 | 0.191 0.194 0.197 0.203 0.204 0.229 0.232 0.234 0.235 0.244 0.269 0.289 0.308 0.329 0.378 0.431 0.441 0.492 0.497 | 0.027 0.015 0.011 0.048 0.039 0.075 0.112 0.038 0.052 0.035 0.022 0.119 0.066 0.105 0.265 0.083 0.103 0.065 0.159 |
| Complex4 |  |  |  |  |  |
| Pro18 Arg7 Gln1 Arg9 Tyr42 Gln6 Lys73 His17 His44 Leu19 Ser72 Lys76 Pro75 Lys5 Lys11 Ile74 Phe41 | 0.179 0.190 0.195 0.200 0.218 0.223 0.229 0.239 0.247 0.275 0.287 0.302 0.390 0.419 0.448 0.454 0.496 | 0.011 0.028 0.025 0.049 0.029 0.047 0.046 0.028 0.050 0.044 0.131 0.196 0.159 0.082 0.228 0.118 0.023 | Lys5 Arg9 Lys73 Gln1 Ile74 Pro75 Leu10 Lys8 His44 Ser72 Ser12 Tyr42 Ala2 Glu46 | 0.184 0.185 0.203 0.235 0.237 0.240 0.260 0.310 0.331 0.430 0.458 0.464 0.488 0.492 | 0.012 0.018 0.021 0.069 0.024 0.029 0.062 0.121 0.125 0.043 0.172 0.168 0.049 0.081 |

Supplementary table 4: the composition of molecular systems used for MD simulations

|  | Number of BMP2 dimers | Number of HS-hexamer molecules | Number of Na+ ions | Number of water molecules | Total number of atoms in the system | Initial box size, Å3 |
| --- | --- | --- | --- | --- | --- | --- |
| BMP2_I_complex1 | 1 | 1 | 3 | 16796 | 54118 | 93×87×68 |
| BMP2_I_complex2 | 1 | 1 | 3 | 13998 | 45724 | 92×88×69 |
| BMP2_I_complex3 | 1 | 1 | 3 | 14549 | 47377 | 86×84×66 |
| BMP2_I_complex4 | 1 | 1 | 3 | 14471 | 47143 | 86×83×66 |
| BMP2_J_complex1 | 1 | 1 | 3 | 15282 | 49576 | 91×89×75 |
| BMP2_J_complex2 | 1 | 1 | 3 | 14369 | 46837 | 92×77×67 |
| BMP2_J_complex3 | 1 | 1 | 3 | 15119 | 49087 | 85×83×70 |
| BMP2_J_complex4 | 1 | 1 | 3 | 14351 | 46783 | 85×84×66 |

REFERENCES:

Henriet, E., Jäger, S., Tran, C., Bastien, P., Michelet, J. F., Minondo, A. M., . . . Vivès, R. R. (2017). A jasmonic acid derivative improves skin healing and induces changes in proteoglycan expression and glycosaminoglycan structure. Biochim Biophys Acta Gen Subj, 1861(9), 2250-2260.

Laguri, C., Sadir, R., Gout, E., Vivès, R. R., & Lortat-Jacob, H. (2022). Preparation and Characterization of Heparan Sulfate-Derived OligosaccharidesOligosaccharides to Investigate Protein–GAG Interaction and HSHeparan sulfate (HS)BiosynthesisBiosynthesis EnzymeEnzymesActivity. In K. Balagurunathan, H. Nakato, U. Desai & Y. Saijoh (Eds.), Glycosaminoglycans: Methods and Protocols (pp. 121-137). New York, NY: Springer US